Chapter 17

  - Introduction

- Corrosion(deteriorative loss of a metal as a result of dissolution environmental reactions.

- Ceramic materials are relatively resistant to deterioration, which usually occurs at elevated temperatures.

- Degradation(a term used to denote the deteriorative processes that occur with polymeric materials.

- May dissolve when exposed to a liquid solvent.

- May absorb the solvent and swell.

- Electromagnetic radiation (primarily ultraviolet) and heat may cause alteration in their molecular structure.

** Corrosion in Metals**

- Corrosion(the destructive and unintentional attack of a metal.

- It is electrochemical and ordinarily begins at the surface.

  - Electrochemical Considerations

- Electrochemical(a chemical reaction in which there is transfer of electrons from one chemical species to another.

- Oxidation(the removal of one or more electrons from an atom, ion, or molecule.

- M(Mn+ + ne-

- Anode(gives up electrons

- Reduction(the addition of one or more electrons to an atom, ion, or molecule.

- Mn+ + ne-(M

- Cathode(accepts electrons.

- Half-Reactions(the individual oxidation and reduction reactions.

- There can be no net electrical charge accumulation from the electrons and ions.

- Electrode Potentials

- Galvanic Couple(two metals electrically connected in a liquid electrolyte wherein one metal becomes an anode and corrodes while the other acts as a cathode

- Electrolyte(a solution through which and electric current may be carried by the motion of ions.

- An electric potential or voltage will exist between the two cell halves, and its magnitude can be determined if a voltmeter is connected in the external circuit.

- Standard Half-Cell(an electrochemical cell consisting of a pure metal immersed in a 1M aqueous solution of its ions, which is electrically coupled to the standard hydrogen electrode.

- The Standard EMF Series

- Standard Hydrogen Electrode(consists of an inert platinum electrode in a 1 M solution of H+ ions saturated with hydrogen gas that is bubbled through the solution at a pressure of 1 atm and a temperature of 25oC.

- Electromotive Force (emf) Series(a ranking of metallic elements according to their standard electrochemical cell potentials.

- Metals at top are noble, or chemically inert, where metals at bottom are more active, more susceptible to oxidation.

- (Vo = Vo2 – Vo1

- (+) (Vo(spontaneous reaction.

- (-) (Vo(no reaction.

- Influence of Concentration and Temperature on Cell Potential

- Nerst Equation

- (V = (Vo- (RT/nF)ln([oxidation]/[reduction])

R = 8.3451 J/mol K

n = number of electrons

F = 96,500 C/mol

- At room temperature (T = 25oC)

(V = (Vo-(0.0592/n)log([anode]/[cathode])

- The Galvanic Series(a ranking of metals and alloys as to their relative electrochemical reactivity in seawater.

- Essentially all metals occur in nature as compounds.

- Exceptions are gold and platinum because, for them, oxidation in most environments is not favorable, and, therefore, they may exist in nature in the metallic state.

  - Corrosion Rates

- Corrosion Penetration Rate (CPR)(thickness loss of material per unit of time as a result of corrosion; usually in terms of mils per year or millimeters per year.

# CPR = KW/(At

W = weight loss

( = density

A = exposed area

K = constant

t = time

- r = i/nF

r = rate (mol/m2s)

i = current (Amps)

n =  number of electrons

F = 96,500 C/mol

17.5	Passivity(the loss of chemical reactivity, under particular environmental conditions, by some active metals and alloys.

- Displayed by Chromium, Iron, Nickel, Titanium, and many of their alloys.

- Passive behavior results from the formation of a highly adherent and very thin oxide film on the metal surface, which serves as a protective barrier to further corrosion.

  - Environmental Effects

- In most instances, increasing fluid velocity enhances the rate of corrosion due to erosive effects.

- The rates of most chemical reactions rise with increasing temperature.

- Increasing the concentration of the corrosive species (H+ in acids) in many situations produces a more rapid rate of corrosion.

- For materials capable of passivation, raising the corrosive content may result in an active-to-passive transition, with a considerable reduction in corrosion.

- A cold-worked metal is more susceptible to corrosion than the same material in an annealed state.

  - Forms of Corrosion

- Uniform Attack(a form of electrochemical corrosion that occurs with equivalent intensity over the entire exposed surface and often leaves behind a scale or deposit.

- Oxidation and reduction reactions occur randomly over the surfaces.

- Probable the most common form of corrosion.

- Examples:

- Rusting of steel and iron.

- Tarnishing of silverware.

- Galvanic Corrosion(occurs when two metals or alloys having different compositions are electrically coupled while exposed to an electrolyte.

- The less noble or ore reactive metal in the particular environment will experience corrosion; the more inert metal, the cathode, will be protected from corrosion.

- The Galvanic Series

- When two alloys are coupled in seawater, the one lower in the series will experience corrosion.

- Generally, the base metal is the same for alloys within the brackets, and there is little danger of corrosion if alloys within a single bracket are coupled.

- The rate of galvanic attach depends on the relative anode-to-cathode surface areas that are exposed to the electrolyte.

- The rate is related directly to the cathode-anode area ratio(for a given cathode area, a smaller anode will corrode more rapidly than a lager one.

- Corrosion rate depends on current density.

- A high current density results for the anode when its area is small relative to that of the cathode.

- Reducing the effects of galvanic corrosion.

- If coupling of dissimilar metals is necessary, choose two that are close together in the galvanic series.

- Use an anode area as large as possible.

- Electrically insulate dissimilar metals from each other.

- Cathode Protection(electrons are supplied to the structure to be protected from an external source such as another more reactive metal or a DC power supply.

- Crevice Corrosion(occurs within narrow crevices and under deposits of dirt or corrosion products.

- Occurs where the solution becomes stagnant and there is localized depletion of dissolved oxygen.

- The crevice must be wide enough for the solution to penetrate, yet narrow enough for stagnancy.

- In many aqueous environments, the solution within the crevice has been found to develop high concentrations of H+ and Cl- ions, which are especially corrosive.

- Many alloys that passivate are susceptible to crevice corrosion because protective films are often destroyed by the H+ and Cl- ions.

- Crevice corrosion may be prevented by:

- Using welded instead of riveted or bolted joints.

- Using nonabsorbing gaskets when possible.

- Removing accumulated deposits frequently.

- Designing containment vessels to avoid stagnant areas and to ensure complete drainage.

- Pitting(a form of very localized corrosion wherein small pits or holes form, usually in a vertical direction.

- Pitting is an extremely insidious type of corrosion, often going undetected and with very little material loss until failure occurs.

- Oxidation occurs within the pit itself, with complementary reduction at the surface.

- Gravity causes the pits to grow downward, the solution at the pit tip becoming more concentrated and dense as pit growth progresses.

- A pit may be initiated by a localized surface defect such as a scratch or a slight variation in composition.

- Polished surfaces display a greater resistance to pitting corrosion.

- Intergranular Corrosion(occurs preferentially along grain boundaries for some alloys and in specific environments.

- The net result is that a macroscopic specimen disintegrates along its grain boundaries.

- Especially prevalent in some stainless steels.

- Weld Decay(intergranular corrosion that occurs in some welded stainless steels at regions adjacent to the weld.

- Stainless steels may be protected from intergranular corrosion by:

- Subjecting the sensitized material to a high-temperature heat treatment in which all the chromium carbide particles are redissolved.

- Lowering the carbon content below 0.03% C so that carbide formation is minimal.

- Alloying it with another metal such as niobium or titanium, which has a greater tendency to form carbides than does chromium so that the Cr remains in solid solution.

- Selective Leaching(found in solid solution alloys and occurs when one element or constituent is preferentially removed as a consequence of corrosion processes.

- Erosion-Corrosion(the combined action of chemical attach and mechanical abrasion or wear as a consequence of fluid motion.

- Harmful to alloys that passivate by forming a protective surface film.

- the abrasive action may erode the film and leave an exposed metal surface.

- Relatively soft metals are sensitive to erosion-corrosion.

- Identified by surface grooves and waves having contours that are characteristic of the flow of the fluid.

- Influence on the corrosion

- Increasing fluid velocity enhances the rate of corrosion.

- A solution is more erosive when bubbles and suspended particulate solids are present.

- Commonly found in piping in positions where the fluid changes direction or flow suddenly becomes turbulent.

- Propellers, turbine blades, valves, and pumps are susceptible to erosion-corrosion.

- Ways to reduce erosion-corrosion

- eliminate fluid turbulence and impingement effects.

- Removal of particulates and bubbles from the solution.

- Stress Corrosion(a form of failure that results from the combined action of a tensile stress and a corrosion environment.

- It occurs at lower stress levels than are required when the corrosion environment is absent.

- Other ways stress corrosion occurs

- From a residual stress that results from rapid temperature changes and uneven contraction.

- In two phase alloys, each phase has a different coefficient of expansion

- Gaseous and solid corrosion products that are entrapped internally cause internal stresses.

- Reducing stress corrosion

- Lower the magnitude of the stress

- Reduce the external load

- Increase the cross-sectional area perpendicular to the applied stress.

- Heat treatment to anneal out any residual thermal stresses.

- Hydrogen Embrittlement(the loss or reduction of ductility of a metal alloy (often steel) as a result of the diffusion of atomic hydrogen into the material.

- A.K.A.

- hydrogen-induced cracking

- hydrogen stress cracking

- In response to applied or residual tensile stresses, brittle fracture occurs catastrophically as cracks grow and rapidly propagate.

- Hydrogen-induced cracks are most often transgranular, although intergranular fracture is sometimes observed.

- Protection may lead to the initiation or enhancement of hydrogen embrittlement.

- For hydrogen embrittlement to occur, a source of hydrogen must be present and the possibility for the formation of its atomic species.

- Pickling of steels in sulfuric acid

- Pickling(procedure used to remove surface oxide scale from steel pieces by dipping them in a vat of hot, dilute sulfuric or hydrochloric acid.

- Electroplating

- The presence of hydrogen-bearing atmospheres at elevated temperatures.

- Reducing hydrogen embrittlement

- reducing the tensile strength of the alloy via a heat treatment.

- Removal of the source of hydrogen.

- “Baking” the alloy at an elevated temperature to drive out any dissolved hydrogen.

- Substitution of a more embrittlement resistant alloy.

  - Corrosion Environments

- Atmosphere

- Aqueous solutions

- Soils

- Acids

- Bases

- Inorganic solvents

- Molten salts

- Liquid metals

- Human body

  - Corrosion Prevention

- Techniques

- Material selection

- Environmental alteration

- Design

- Coatings

- Cathodic Protection

- Inhibitor(a chemical substance that, when added in relatively low concentrations, retards a chemical reaction.

- Normally used in closed systems such as automobile radiators and steam boilers.

- Cathodic Protection(a means of corrosion prevention whereby electrons are supplied to the structure to be protected from an external source such as another more reactive metal or a DC power supply.

- Galvanic Couple( the metal to be protected is electrically connected to another metal that is more reactive in the particular environment.

- Sacrificial Anode( an active metal or alloy that preferentially corrodes and protects another metal or alloy to which it is electrically coupled. Magnesium and zinc are commonly used.

- DC power supply

- The negative terminal of the power source is connected to the structure to be protected.

- The other terminal is joined to an inert anode (often graphite) which is buried in the soil.

- A current path exists between the cathode and anode through the soil.

3. Cathodic protection is used in preventing corrosion in water heaters, underground tanks and pipes, and marine equipment.